## Slide 1: New features in Polymer Genome & Development Status
Chiho Kim Materials Science & Engineering, Georgia Institute of Technology

## Slide 2: OVERVIEW
Feature engineering tool
Predictor
ML model generator
Genetic algorithm toolkit
Utilities
Polymer fingerprint generator
Polymer Genome
Output - Atomic / block / chain level fingerprints
Input - SMILES
RFE
PCA
LASSO
One hot encoding
Linear regression
GPR
Learning curve
Duplication checker
+ more tools

## Slide 3: NEW FEATURES
Genetic algorithm toolkit
  Available on Gaanam2,3,4 and Tyrion2.
  Currently, applicable only for polymer design, but will be generalized.
Polymer fingerprinting API
  {.json} in, {.json} out
  Can be used in any languages (useful for end-users)
Updates on polymer fingerprinting
  ‘Short’ polymer issue fixed
  Added a new tag for ‘skipping’ side-chain related descriptors
Feature engineering tool
  Added LASSO for feature elimination

## Slide 4: GENETIC ALGORITHM TOOLKIT
Genetic algorithm
Method for solving optimization problems based on natural selection, the process that drives biological evolution.
B11
B12
B13
B14
P1
B21
B22
B23
B24
P2
B11
B12
B21
B22
B11
B12
B23
B24
B21
B22
B13
B14
B21
B22
B11
B12
B11
B12
B21’
B22
B21
B22
B13
B14’
B21
B22’
B11
B12
C1
C2
C4
C3
Not mutated
Genome breakdown position
Crossover
Mutation
Parents
Children
Repeat
Selection
Crossover
Mutation
Fitness function (evaluation)
Parents
Children
Generate Initial population
Fitness function (evaluation)
Start

## Slide 5: GENETIC ALGORITHM TOOLKIT
Generation
1
10
100
Bandgap, predicted (eV)
4
6
8
10
12
Eg = 6 eV
Average
Parent polymers
Maximum
Average
Minimum
Offspring polymers
Generation
1
10
100
500
600
700
400
Glass transition temperature, predicted (K)
Tg = 500 K
Eg = 8.2 eV / Tg = 558 K
Eg = 9.3 eV / Tg = 546 K
Eg = 9.1 eV / Tg = 552 K
NH
*
*
N
*
*
F
F
F
O
OH
OH
HO
*
*
F
F
F
NH
Application example
Goal – to design polymers with Tg>500 K & Eg>6 eV
Genome – polymer building blocks
ex) -CC-, -C6H4- …(~3,000 retrosynthetic fragments)
PC1
PC2
1st generation
10th generation
100th generation
50th generation

## Slide 6: API-BASED POLYMER FINGERPRINTING
API server
</CODE>
SMILES, API key
Polymer fingerprint
{.json}
Benefit of API Application programming interface
Easy to bind to end-user’s codes
Language-agnostic
Not need to create fp_input
Not need to connect to G2, G3, G4, T2
1 2 3 4 5 6 7 8 9 10 11 12 | ﻿import requests import pprint url = 'http://api-server-address/' myJsonInput = { 'API-Client-Id':'******', 'API-PWD':'******', 'SMILES': 'CCC(CCCC)CCOCCCCOC'} result = requests.post(url, params=myJsonInput) pprint.pprint(result.json())
Example code
﻿In [1]: runfile('API-Caller.py') {'afpC4_C4_C4': 0.25, 'afpC4_C4_H1': 1.0454545454545454, 'afpC4_C4_O2': 0.09090909090909091, 'afpC4_O2_C4': 0.045454545454545456, 'afpH1_C4_H1': 0.3409090909090909, 'afpH1_C4_O2': 0.18181818181818182, 'bfp197': 0.8181818181818182, ... 'mfpNumAliphaticRings': 0.0, 'mfpNumAromaticRings': 0.0, 'mfptpsa': 0.10488636363636364}

## Slide 7: UPDATES ON POLYMER FINGERPRINTING
What’s the issues?
  ‘Short’ polymer problem
  Side-chain related descriptors
fp([*]C[*]) ≠ fp([*]CC[*])
fp returns wrong result for short polymers (main chain length < 2) like ([*]C[*])  Fixed
# | key | definition
21 | side_chain_abs | Absolute length of the shortest side chain
22 | side_chain_large_abs | Absolute length of the longest side chain
fp takes too long computation time for complex polymers
To bypass use a tag compute_side_chain = 0

## Slide 8: LASSO FOR FEATURE ELIMINATION
LASSO least absolute shrinkage and selection operator
A regression analysis method that performs both variable selection and regularization in order to enhance the prediction accuracy and interpretability of the statistical model it produces.
See the movie that shows how LASSO simplifies regression model by eliminating silly descriptors  https://www.youtube.com/watch?v=NGf0voTMlcs
file_fp_prop = fp_prop.csv
col_X = aT bT m e
col_Y = DFT_bandgap
job = LASSO
LASSO_n_fold = 5
LASSO_col_X_keep = afp_C4_C4_C4 bT
LASSO_file_fp = fp_prop_LASSO.csv
verbosity = 1
Input for fe to run LASSO

## Slide 9: DEVELOPMENT STATUS
Underway
  Ladder polymer – Polymer drawer, fingerprinting & dataset
  Block level polymer fingerprinting – completeness, uniqueness & minimal
  Documentation (GA)
Staggering
  Side-chain related fingerprinting algorithm – staggering
  Polymer Genome Webserver – mirroring site (backup for emergency)
  Data mining & curation & model development –
Intrinsic_viscosity_eta
Specific_volume
Crystallization_temp.
Surface_tension
Linear_expansion_coefficient
Gas_solubility_coefficient_(S)
Contact_angle
Volume_expansion_coefficient
Softening_temp.
LC_phase_transition_temp.
Water_absorption
Gas_diffusion_coefficient_(D)
Melt_viscosity